## Slide 1
Review of previous classes
1. Nanotechnology in upward motion: next future of science and technology is nanotechnology
2. Constructive - Destructive interference by thin films
3. Non-Reflective Surfaces
4. Super-Hydro-Phobicity
5. Self-Cleaning
Nano in Histroy
The Localized Surface Plasmon Resonance
DICHROISM
Development of nanoscience and technology
Diversity of nano field
Surface to volume atoms of Cuboctahedral system
M(K) = (1/3)*(10K3+15K2+11K+3), K = No. of shell
NK =10K2 + 2, Every shell contains number of shell
SIZE EFFECT
Quantum Effect
Colour, Melting point, Specific heat, Electrical, Magnetic properties etc.
To-Down Method of Preparation
Ball mill, Thermal, Arc discharge, Laser ablation etc. Lithography
Bottom – up preparation method
Characterization: AFM, STM, TEM, SEM, IR, Raman, XRD etc.
Carbon Nanotube
Energy at Nanoscale, Nanomechanics, Nanoelectronics, Application etc.

## Slide 2
CARBON NANOTUBE
Allomorphs of carbon are depicted. (a) Diamond forms in a tatrahedral (sp3 bonding) arrangement where each carbon is bonded to four others. (b) Graphite is the most stable form of carbon. It forms in planes that consist of hexagonal arrangement of carbon atoms. The bonding in graphite is sp2. Van der Waals forces hold the planes together. (c) Another form of diamond called lonsdaleite has more hexagonal character to its structure. It is believed to form after a meteor impact that transforms graphite into lonsdaleite while creating the hexagonal form of graphite. (d)–(f) Fullerenes were discovered in 1985 by Richard Smalley and his group. Fullerenes are carbon’s representative in the zero-dimensional class of nanomaterials. (g) Amorphous carbon does not have any crystalline structure (no longrange order). Much of amorphous carbon contains small domains of crystalline graphite (also called turbostratic graphite) with some level of amorphous carbon that holds them together.
Coal and soot are amporphous carbons. (h) Carbon nanotubes are called fullerene pipes and comprise (arguably) one of the most remarkable of the carbon allotropic class of materials—or of all materials, for that matter. Glassy carbon is a nongraphitizing carbon that is used in electrodes and for high-temperature crucibles. Glassy carbon is a purely isotropic form of graphite. Carbon nanofoams are considered to be an allomorph of carbon that consists of a three-dimensional structure of carbon clusters. Nanofoams were discovered in 1997 by A. V. Rode et al.
(a)
(b)
(c)
(d)
(e)
(f)
(g)
(h)

## Slide 3
A SINGLE GRAPHITE SHEET: GRAPHENE
An example of mono-dimensional system

## Slide 4
The unit cell of graphite (containing two atoms) is shown on the left. On the right, the relationship between two planes of graphite is depicted.

## Slide 5
Three layers of graphite are shown. The d-spacing between layers is 3.34 A. The lattice parameter a of the unit cell is equal to 2.46 A. The C–C bond length is 1.42 A.
bc–c= 1.42 Å
c = 6.708 Å
a = 2.46 Å
d = 3.34 Å

## Slide 7
ELECTRONIC STRUCTURE of GRAPHITE
In 3D graphite the inter-planar interactions are weak with respect to the in-plane C-C interactions
The electronic structure of 2D graphite is similar (in first approximation) to that of 3D graphite
The  e * bands of graphene “touch” in 6 points (at the corners of hexagonal Brillouin zone ) and equal the Fermi energy for one
special wavevector
K- POINT

## Slide 8
Nc =Odd ( example 3, 11, 15, 19 and 23, sp hybridization, linear or ring structure-> abundance-> tetrahedral bond angles )
Nc = even= cage structures
Nc = 30 -40 - > no stable structure
Nc >40 -> fullerene, C60, C70, C80, C90 etc.
Nc = 60-> 90 edges, 32 faces (12 are pentagons and 20 hexagones) and 60 vertices
Euler’s theorem to polyhedra, f+v=e+2, f = face, v = vertices, e = edges
Diameter = 7.10A, Pentagon has no double bond (bond length = 1.46A. Hexagon has alternate double bonds with bond length 1.40A. (Graphite has only hexagon with bond length 1.42A)

## Slide 9
A fulleride crystal is displayed. The crystal shown is an fcc type within which van der Waals gaps separate the constituent fullerenes. Intercalation of metals like lithium between and among fullerenes occurs to form stable complexes.

## Slide 10
Formation of single adduct (single functional) fullerenes: Each fullerene has 30 p-bonds, many of which are available for supramolecular synthesis, which involves intermolecular interactions. All functionality provided for a chemically modified fullerene in this figure occurs at a single addend attached to the fullerene with covalent bonds. The purpose of the addend is to modify the fullerene with a chemical moiety that provides: (1) an anchor substituent between the fullerene and a metal surface, and (2) a means to interlink with other fullerenes derivatized in the same way or in different ways. The mono adduct contains
thiol groups for bonding to a gold surface and carboxylic acid groups to provide intermolecular bonding (via hydrogen bonds) between fullerenes and the pi−pi interaction capability.
Br
Br

## Slide 11
A two-dimensional array of fullerenes (modifi ed as pictured in previous Fig.) on gold substrate is shown. Along the lateral (x) axis, modifi ed fullerenes are held together by hydrogen bonds between carboxylate functionalities. Along the longitudinal (y) axis, fullerenes are attracted to each other via p−p interactions. Molecular models have confirmed the viability of such a system.

## Slide 12
C60 dimer formed by [2 + 2] cycloaddition. The structures are formed during prolonged exposure to UV or laser light. The dimers (and higher forms) are insoluble in solvents that buckyballs normally disperse. The dimers revert to individual C60 molecules by heat treatment under ambient pressure conditions.

## Slide 13
Generic C60 arrays are shown: Top left: rhombohedral; top right; tetrahedral; and bottom: linear orthorhombic polymers. Red lines represent chemical linking groups. Blue squares represent fullerene dimer linkage. Three-dimensional arrays are also possible.

## Slide 15
TWO DIFFERENT CLASSES
S. Iijima Nature 354: 56 (1991)
Dext.= 20÷200 Å
Dint. = 10÷100 Å
Multi-wall (MWNTs)
Single-wall (SWNTs)
D = 10÷20 Å
S. Iijima, T. Ichihashi Nature, 363: 603 (1993)

## Slide 16: PROPERTIES
ELECTRONIC
MECHANICAL
CHEMICAL
THERMAL
OPTICAL
MAGNETIC
SPINTRONICS

## Slide 17
High chemical stability (inertness against oxidation..)
Structural integrity after intercalation and de-intercalation
High performances of gas storage
Feasibility to attach foreign species or chemical groups
Thermal stability (up to 2000 C under vacuum)
Low density (1.33-1.40 g/cm3) (1/6 the weight of steel)
Mechanical Resistance (Young modulus ~1.8 TPa)
Breaking strength : 13-50 GPa (a strain of 6%)
Volume compressibility : 2 x 10 –3 1/kbar
Reversible deformation modes (bending, axial compression, torsion)
The highest thermal conductivity (2000-6000 W/m·K)
Metallic or semiconducting behaviour
Electrical conductivity (1 GA/cm2 )
High efficiency of Field Emission (FE)

## Slide 18
HOW TO ROLL GRAPHENE

## Slide 19
Sketch of the way to make a single-wall carbon nanotube, starting from a graphene sheet
The various ways to roll graphene into tubes are therefore mathematically defined by the vector of helicity Ch, and the angle of helicity θ, as follows
where n and m are the integers of the vector OA considering the unit vectors a1 and a2.
The vector of helicity Ch(= OA) is perpendicular to the tube axis, while the angle of helicity θ is taken with respect to the so-called zig-zag axis, i. e., the vector of helicity that makes nanotubes of the “zig-zag” type . The diameter D of the corresponding nanotube is related to Ch by the relation:
a1=a2=2bcos30
bond=a/√3

## Slide 20
Illustration of nanotube structure and the chiral vector. The dark arrows represent the tube axes of zigzag and armchair tubes. The arrow in the middle represents the tube axis for chiral tubes, the vector sum of the others.
because of the six fold symmetry of the graphene sheet, the angle of helicity θ for the chiral (n,m) nanotubes is such as 0<θ<30◦

## Slide 21
Sketch of three different SWNT structures as
examples for (a) a zig-zag-type nanotube, (b) an armchair type nanotube, (c) a helical nanotube
(a)
(b)
(c)
Image of two neighboring chiral SWNTs within a SWNT bundle as seen by high resolution scanning tunneling microscopy
(10,10)
(10,5)

## Slide 22
The translational unit cell of a (10,0) zigzag tube is shown below. The width of the cell is equal to √3a, where a is the unit vector for the graphene lattice. The translational unit cell for a (6,6) armchair tube is shown below. The width of this unit cell is equal to the unit vector a of the graphene lattice . Chiral tubes that have lower symmetry are characterized by larger cells than the two depicted in the fi gure. The magnitude of the chiral vector is the circumference of the tube. The magnitude of the translational vector is the width of the cell. The chiral vector (along the circumference) and the translational vector (along the tube axis) are orthogonal to one another.

## Slide 23
SWNTs are either electrically semiconducting or electrically conducting (metallic). Semiconducting SWNTs are represented by solid green dots and conducting tubes by hollow purple dots. Tubes are conducting if (m – n) or (n – m) is a multiple of 3: n – m = 3q, where q is an integer. Therefore, all armchair tubes are metallic, all zigzag tubes with n a multiple of 3 are conducting, and all chiral tubes that fall into the general category of n – m = 3q are conducting as well.

## Slide 24
Making (10,0) and a (5,5) carbon nanotubes by folding a graphene transparency.

## Slide 25
SWNTs represent the ideal 1D QUANTUM WIRE
The transport properties are dependent on the geometrical characteristics: HELICITY -DIAMETER
Depending on the structure the nanotubes can
have a metal-like or semiconducting behaviour
The electrons are confined along the circumference and propagate exclusively along the axis of the cylinder . The conduction is ballistic.

## Slide 26
A set of 1D energy states, corresponing to sections of the band structure of 2D graphite .
kc·Ch=2pj
Confinement of electrons along the tube circumference
SEMICONDUCTOR
ELECTRONIC STRUCTURE of SWNT
Depending on the position of allowed wavevector with respect to k-point
METAL-LIKE

## Slide 27
The nanotubes (n,n) and (n,m) with n-m=3i behave as 1D metals : the density of states at the Fermi level has a finite value.
(n,n)
(n,m) | n-m or m-n =3i
Metal-like Nanotubes (zero-gap)
In metal-like SWNTs the conduction is due to discrete 1-D electronic states (spaced of about 0.4 meV) which extend along the whole tube length
All arm chair CNT are conducting as n-m=0 for all arm chair
(6,0), (9,0), (12,0) -> Zigzag tubes are metallic. Others semiconducting
(6,3), (6,9), (6,12)-> Chiral CNT are conducting

## Slide 28
Dependance of the gap on the diameter
Eg~1/R,
0.2  Eg  1.2 eV
(n,m) | n-m3i
T.W. Odom, J.L. Huang, P. Kim e C.M. Lieber, Nature 391 (1998): 62
DOS= 0 at the Fermi level
Semiconducting Nanotubes
The gap decreases with diameter increasing .

## Slide 29
Mechanical Properties of Materials
Breaking carbon nanotube is mostly by breaking a bunch of C-C or C=C or combination.
SP2-SP3 covalent bonds are the strength of the carbon nanotube
The specific strength of carbon nanotubes is the order of 48.5 x 103 kN.m.kg-1
Steel ~ 1.54x102Gpa

## Slide 30
What is the theoretical tensile strength σs in gigapascals (1GPa = 109Nm2) of carbon – carbon bonds of different order? Assume that all bonds stretch to 2.5xtheir respective length before breaking. How much mass under earth’s gravitational pull are these bonds able to hold without breaking?
Type | Bond order | Bond length, L (nm) | Bond dissociation energy (Ebde) (kJ.mol-1) | Bond break length, d = 2.5L-L(nm)
C-C | 1.0 | 0.154 | 348 | 0.231
C=(onepi+onecovalent) C | ~1.33 | 0.142 | 480 | +213
C= (two co-valent) | 2.0 | 0.134 | 614 | +0.201
C≡C | 3.0 | 0.120 | 839 | 0.180
Bond dissociation energy=
Force Required =
The covalent radius rc of a carbon atom is 0.077nm-the cross-sectional area Ac = πr2 = 3.1416x(0.077x10-9m)2=1.86x10-20m2
The tensile strength σ (1Pa=N.m-2) of one C-C bond =
The maximum force Fmax that one C-C bond is able to hold without breaking is the product of the tensile strength and the area of the material AM (e.g. the diameter of the tube). If only one C-C bond, then Fmax = Amσ = Acσ=2.50x10-9N. Mmax=(F/g)=2.54x10-10kg

## Slide 31
Type | Bond dissociation energy (Jx10-19) | Force F (Nx10-9) | Tensile strength σ(Gpa) | Mass mmax (kgx10-10)
C-C | 5.78 | 2.50 | 134 | 2.54
C=(onepi+onecovalent) C | 7.97 | 3.74 | 201 | 3.82
C= (two co-valent) | 10.2 | 5.07 | 272 | 5.18
C≡C | 13.9 | 7.74 | 416 | 7.90
The tensile strength increases with the bond strength. Therefore, theoretical limit of the tensile strength of one of the strongest bonds in nature is quite high. If the mass of two carbons in the bond is 1.99x10-26kg, these bonds can hold about 1015-1016 times their own mass.

## Slide 32
Electrical: One dimentional nanomaterials -> pseudo-one dimentional nanomaterials.
Due to confinement -> electrical conduction is quantized
Resistivity in CNT is constant. So CNT are excellent materials for high current applications. Theoretically 1000 times more than that of silver or copper.
Thermal Properties: Along the tube axis, carbon nanotubes have excellent thermal conductivity to the tune of~6000W.m-1.K-1 at room temperature. Copper->385Wm-1K-1
Along the diameter of the tube, carbon nanotube are insulating
Thermal stability of carbon is very high ~3100K in vacuum

## Slide 33
Metallic CNT has no band gap. Semiconducting CNT have a band gap i.e. function of diameter. The band gap ranges from 0.4 to 0.7eV.
Eg is the band gap in electron volts. W is the tight binding energy (2.7±0.1eV), and b is the bond length
The difference is best illustration in DOS plots. The DOS is a function of the number of quantum states in the energy range between E and E+dE devided by the product of dE and the volume of the sample. In a metal, the Fermi level is populated and therefore the DOS shows a positive population in that area. For a semiconductor, the Fermi level (technically, the chemical potential) is empty (the band gap), and the DOS in that region has zero population (nostates). As energy is increased on either side, peaks valled van Hove singularities appear. These regions are responsible for the optical properties of carbon nanotubes (e.g., transition between the von Hove singularities).
Optical properties of single-walled carbon nanotubes. Van Hove singularities are shown for (a) (9,9) metallic conducting tubes and (b) (11,7) semiconducting tubes. Note that there is no band gap in the metallic tube (all states populated). The semiconducting tube has the region in the center with no populated states. Optical transitions occur between the van Hove peaks.

## Slide 34
Intertube spacing: Armchair: 0.341nm, Zig zag: 0.341nm, Chiral(2n,m):0.339nm